PART 1 - GENERAL

1.1 Summary.

A.  Section includes horizontal product types.

1.  Wainscoting
		2.  Wall Cladding

3.  Tub and shower enclosures

1.2 Definitions

A.  Solid surface sheets are non-porous, homogeneous, hygienic, renewable  	  	      materials which consist of acrylic resins, ATH mineral fillers and pigments.

1.3 Submittals

A.  Meganite Product Data

1.  Meganite color chart

2.  MSDS sheets

3.  Product Description to include identifying name and color

B.  Shop Drawings

1.  Indicate plans, dimensions, elevations, layout, cutouts, accessories, 			     support or reinforcements, gloss levels, and edge treatments.

C.  Samples of final color selection, minimum 2” x 2” to be retained as standard.
	D.  Manufactures Fabrication and Installation Manual

1.4 Quality Assurance

A.  Fabricator and Installer qualifications

1.  Firms must employ skilled craftsmen with experience for the 			                 applications required for this project.

2. Firms must be certified by the local master distributor.

B.  Applicable Standards

1.  Unless otherwise indicated materials must meet industry standards as 		                   referenced herein:

a. American National Standards Institute (ANSI),

b. National Electrical Manufacturers Association (NEMA),

c. American Society for Testing and Materials (ASTM)

C.  Source Limitations

1.  Obtain all materials from single master distributor source.

D.  Mockups

1.  Where required the specified may require mockups to verify selections, 	                  edges, bowls, coves, etc. to be used as standard for judging quality.

2.  After approval, mockups may be incorporated into the project to save 	      	                 costs.

3.  Preinstallation Conference.

4.  Conduct conference at project site to comply with requirements.

1.5 Delivery, Storage, Handling

A.  Handle materials according to manufacturer’s instructions,

B.  Stores all components indoors, and provides protective wrapping or crating.

C.  Do not deliver any parts or components to the job site until it is prepared for 	   	      installation.

1.6 Job Site Conditions

A.  Installation sites must be maintained at the ambient temperature and humidity              	as planned for the project for a minimum of 48 hours prior to installation,      	and continuously afterwards.

1.7 Warranty

A.  Provide the manufacture’s 10 year warranty against defects in materials.

1.  Damage caused by abuse, improper manufacturing or installation     	techniques, or neglect will

not to be warranted.

1.8 Maintenance

A.  Provide manufacturer’s recommendations for maintenance.

B.  Provide materials for future repair, if necessary, from the same batch     	or dye lot as the installed products.

PART 2 - PRODUCTS

2.1 Manufacturer

A.  Meganite, Inc					Telephone:  (800) 836-1118

1254 E. Lexington Ave				Fax:             (909) 391-8885

Pomona, CA 91766

www.meganite.com

2.2  Master Distribution Network

| Please check ONE box only | Distributor Name | Contact Information |
| --- | --- | --- |
|  | Aetna Plywood D.R.I.V.E - Dedication * Resource * Inventory * Value-added * Experience | www.AetnaPlywood.com 1-708-343-1515 |
|  | E.B. Bradley Co. First Choice in Quality and Services. | www.ebbradley.com 1-800-533-3030 (California) 1-800-562-8366 (Oregon & Washington) |
|  | Fessenden Hall Servicing the industry for over 120 years. | www.fessendenhall.com 1-800-220-2233 |
|  | Maxstone International People who care. Products that endure. | www.maxstoneusa.com 1-877-778-1149 |
|  | New England Surfaces Premier Interior Surfaces | www.newenglandsurfaces.com 1-800-388-3466 |
|  | Solid Source Exceeding your expectations | www.solidsource.ca 1-800-545-0082 |
| If your distributor is NOT LISTED, please check this box. |  |  |

2.3  Materials

A.  Solid homogeneous sheet blended with acrylic resins, ATH mineral fillers and 	      pigments to comply with industry standardized performance characteristics 	  	      identified below.

B.  Thickness:

1.  ½” thick for both vertical and horizontal applications.

2.  ¼” thick for vertical applications

C.  Select color and design for all surfaces.

1.  Detailed in Schedule of Materials in Section 3

D.  Select edge detail treatment for all surfaces as shown on drawings

1.  Detailed in Schedule of Materials in Section 3

E.  To meet or exceed all Performance Characteristics,

1.  Flame Spread Index <25, in accordance with ASTM E 84, Class 1A

2.  Smoke Developed Index < 25, in accordance with ASTM E 84, Class 		                1A

3.  Stain Resistance to meet ANSI Z-124.3, no effect

4.  Wear and Cleanability to meet ANSI Z-124.3 passes

5.  Fungus Resistance to meet ASTM G21, does not support microbial 	     	                 growth

6.  Bacteria Resistance to meet ASTM G22, does not support microbial 	         	                 growth

7.  Meet NSF 51, approved

8.  Impact Resistance to meet NEMA LD3-3.3, ½ pound ball drop

9.  Color Stability to meet NEMA 3-3.3, no change

10.  Barcol Hardness to meet ASTM D2583, 60

11.  Tensile Strength to meet ASTM D 638, 6000 p.s.i.

12.  Flexural Strength to meet ASTM D790, 9000 p.s.i.

13.  Thermal Expansion to meet ASTM D696, 1.3” 10-6 in/in /°F

14.  Boiling Water Surface Resistance to meet NEMA LB3-3.5, no effect

15.  High Temperature Resistance to meet NEMA 3-3.5, no effect

16.  Water Absorption to meet ASTM D570, 0.04%

17.  Specific Gravity, 1.7

F.  Accessories

1.  Manufacturer’s 2-part approved adhesive to provide non-porous, 	    	                  inconspicuous joints.

2.  Silicone sealant adhesive, color matched to sheet panels.

G.  Fabrication

1.  Fabrication to be completed by a Meganite certified fabricator and 	      	                  installer

a. Fabricated according to current Meganite Fabrication, and 	  	    Industry-Accepted Standards

2.  Fabricate parts and components in manufacturing shop to greatest 	  	     extent practical to size and shapes indicated, in accordance with 	  	      approved shop drawings, and manufactures or industry’s printed 	 	       instructions.

3.  Form joints between compounds using manufacturers’ standard joint 	 	                 adhesive to be inconspicuous and without voids.

4.  Rout and finish all component edges with clean and uniform work.

a. All cutouts must be routed and then sanded for a smooth edge

5.  Repair all defective or inaccurate work.

6.  When applicable, comply with manufacturers thermoforming 	 	     	                  requirements

a. Heat entire piece, (do not spot heat) to a uniform 280° - 325 °

b. Form pieces to shape prior to seaming and joining

c. Sand edges and remove nicks and scratches

d. Prevent blistering, whitening, and cracking during the forming 		                            process.

H.  Vertical Surfaces with silicone sealed seams:

1.  Wall panel material to be seamed with 1/8” wide seam joint using 	     	                  color-matched silicone; adhesively applied to solid substrate.

I.  Vertical Surfaces with hard seams:

1.  Wall panel material to be seamed at seam joint with manufacture’s 		                  color matched joint adhesive without voids; adhesively applied to solid 		       substrate.  Expansion joints to be 1/8” wide filled with color matched 		                    silicone every 10’ to 15’.

K.  Finishing

1.  Surfaces should have a consistent and uniform finish

2.  Select color from standard offering

a. Select finish after reviewing samples.

b  Retention of finish depends upon color selected and the intended 		                use of the  product.

c. Greater polishing will increase cost,

d. Matte finish is the standard.

3.  Provide surfaces with a uniform finish

a. Greater polishing increases cost

1)  Matte is standard and requires least maintenance

1a)  Matte Finish; gloss range 5 - 20

2)  Use Semi-Gloss to bring out depth in darker patterned 			                               materials; semi-gloss will be more expensive and will 			                                require more maintenance

2a)  Semi-Gloss Finish; gloss range 20 – 50.

- Use Polished Finish for Light Duty only.  This is most expensive, and much heavier maintenance requirements.

3a)  Polished Finish: gloss range 50 – 80

PART 3 – EXECUTION

3.1  Examination

A.  Examine substrates where solid surface will be installed with fabricator for 	  	      compliance with tolerances and other conditions at job site.

1.  Coordinate with contractor to correct unsatisfactory conditions.

B. Proceed to complete installation only after all conditions are repaired and 		     acceptable.

3.2 Installation

A.  Install solid surface according to manufacturer’s Fabrication and Installation 		      Manual

1.  Install all components plumb, level, and rigid; scribed to adjacent 		                  surfaces; according to approved shop drawings and product data.

2.  Provide components in largest pieces available for proper installation.

3.  Form field joints using the manufacturure’s approved adhesive, with 		                  joint inconspicuous in finished work.

4.  Cut and finish component edges with clean, sharp returns.

5.  Carefully remove scratches and clean entire surface.

3.3  Repair

A.  Repair or replace any damaged work.

3.4  Clean and Protect

A.  Keep components clean during transportation and installation.

B.  Clean all surfaces according to manufacturers Care and Maintenance Guide

C.  Remove all adhesives, caulks, sealants, etc.

D.  Cover and protect all surfaces to protect from damage until accepted by 		      owner.

3.5  Schedule of Materials

A.  Vertical Applications

1.   Surfaces of material adhesively joined with inconspicuous seams

|  | Location | MEGANITE Product Name & Color Code (EX. Bright White – 001A) |
| --- | --- | --- |

| A | Vertical Thickness |  |
| --- | --- | --- |
| B | Horizontal Thickness |  |
| C | Inlay |  |
| D | Edge Details |  |
| E | Finish |  |